Test Results

Effect of Pelletized Lime on Properties of PG 64-16

	
	
	
	

	Property
	PG 64-16
	PG 64-16 + 20% Pelletized Lime1
	Specification

	Original Binder

	G*/sin  @ 70º C, kPa
	0.62
	0.83
	1.00 min

	Viscosity @ 135º C, cP
	427
	554
	3000 max

	RTFO Binder

	G*/sin  @ 70º C, kPa
	1.46
	2.01
	2.20 min

	PAV (100º C) Binder

	G*sin  @ 34 C, kPa
	1001
	1236
	5000 max

	Creep Stiffness @ -6º C, MPa

Creep Rate @ -6º C
	202

0.309
	210

0.304
	300 max

0.300 min

	Notes:  

1. pelletized lime added % by mass asphalt


