[image: image1.wmf]Available Ca(OH)2

Sample

% Ca(OH)2

Not exposed to air

47.2

48 hours exposure

51.2

3 days exposure

55.9

5 days exposure

51.4

10 days exposure

44.2


